Hot-galvanized product

|  |  |
| --- | --- |
| Type | Characteristics |
| Type of coating | Zinc |
| Aluminum zinc alloy |
| Mode of coating | Zinc coating for double side 60～275g/m2，  Zinc coating of one side 30～137.5g/m2 |
| Aluminum zinc alloy coating 40～275 g/m2(double side) |
| Thickness scope | Steel band thickness: 0.25～1.6mm;  Steel band width：900～1300mm |
| Steel grade | Drawing: common, drawing, deep drawing, ultra deep drawing |
| Cold forming high strength steel: 180～420MPa（yield strength） |
| Structural strength: 220～350MPa （yield strength） |

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| NO. | Grade | size，mm | | Mode of coating g/m2 | standard | Using area |
| thickness | width |
| 1 | DX51D | 0.3～1.6 | 900～1300 | 60～275 | Q/320582 YZL401  JX/YZL C402-2018 | common |
| 2 | S220GD+Z、S250GD+Z、  S280GD+Z、S320GD+Z、  S350GD+Z | 0.3～1.6 | 900～1300 | 60～275 | Structure |
| 3 | DX51D+Z-E | 0.4～1.6 | 900～1300 | 60～275 | Q/320582 YZL401 | Common for home appliances |
| 4 | DX52D+Z  DX53D+Z | 0.3～1.6 | 900～1300 | 60～275 | Q/320582 YZL401 | deep drawing for home appliances |
| 5 | SGCC | 0.3～1.6 | 900～1300 | 60～275 | Q/320582 YZL401 | common |
| 6 | CS TypeA、  CS TypeB | 0.3～1.6 | 900～1300 | 60～275 | Q/320582 YZL401 | common |
| 7 | DX51D+AZ  S250GD+AZ | 0.3～1.6 | 900～1300 | 40～275 | GB/T 2518 | Coating Al-Zn for building |