Electrolytic tin product

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| |  | | --- | | Classification | | |  | | --- | | Type | | |  | | --- | | Code Name | |
| |  | | --- | | Original plate | | - | MR, L, D |
| |  | | --- | | Treatment level | | - | T-2, T-2.5, T-3, T-3.5, T-4, T-5 |
| |  | | --- | | Annealing mode | | |  | | --- | | Continuous Annealing | | CA |
| |  | | --- | | Equidifferent tinning identification method | | |  | | --- | | Heavy tinning surface integral identity | | A |
| |  | | --- | | Light tinning surface  integral identity | | D |
| |  | | --- | | Heavy tinning surface  Side identity | | F |
| |  | | --- | | Light tinning surface  Side identity | | G |
| |  | | --- | | Surface state | | |  | | --- | | Smooth and bright surface | | B |
| |  | | --- | | Stone surface | | R |
| |  | | --- | | Silver surface | | S |
| |  | | --- | | Matte surface | | M |
| |  | | --- | | Surface treatment method | | |  | | --- | | chemical passivation | | CP |
| |  | | --- | | electrochemical passivation | | CE |
| |  | | --- | | low-chrome passivation | | LCr |
| |  | | --- | | Edge shape | | |  | | --- | | straight | | SL |
| |  | | --- | | Thickness of tin | | |  | | --- | | Equal-thickness tin coat | | E |
| |  | | --- | | Equal-thickness tin coat | | D or A |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| No. | Grade | scope | | Standard | Main usage |
| thickness | width |
| 1 | MR-T-2.5CA、MR-T-3CA、MR-T-3.5CA、MR-T-4CA、MR-T-4.5CA、MR-T-5CA | 0.17～0.40 | 800～1220 | GB/T 2520、JIS G 3303、technical protocol | Cans of food、beverages、aerosol、chemical |
| 2 | MR-T-4CA-A、MR-T-4CA-N、MR-T-4CA-Y | 0.17~0.40 | 800～1220 | Q/320582 YZL 501 | Cans of beverages、milk powder |