Electrolytic tin product

|  |  |  |
| --- | --- | --- |
| Classification | Type | Code Name |
| Original plate | - | MR, L, D |
| Treatment level | - | T-2, T-2.5, T-3, T-3.5, T-4,T-4.5, T-5 |
| Annealing mode | Continuous Annealing | CA |
| Surface state |  Smooth and bright surface | B |
| Stone surface | R |
| Silver surface | S |
| Matte surface | M |
| Surface treatment method | Chemical passivation | CP |
| Electrochemical passivation | CE |
| Low-chrome passivation | LCr |
| Edge shape | straight | SL |
| Thickness of tin | Equal-thickness tin plating | E |
| Differential thickness tin plating | D或A |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| No. | Grade | Scope | standard | Main usage |
| thickness | width |
| 1 | MR-T-2.5CA、MR-T-3CA、MR-T-3.5CA、MR-T-4CA、MR-T-4.5CA、MR-T-5CA | 0.17～0.40 | 800～1220 | GB/T 2520JIS G 3303technical protocol | Cans of food、beverages、aerosol、chemical |
| 2 | MR-T-5CA-A、MR-T-4CA-N、MRT3.5CA-Y、MR-T-4CA-Y、MR-T-5CA-Y、MR-T-4CA-P、MR-T-5CA-P、MR-T-5CA-B | 0.17~0.40 | 800～1220 | Q/320582YZL 501 | Cans of beverages、milk powder etc |